## Slide 1: Measurement of fundamental ion-atom interaction parameters for heavy ion beam materials analysis
Mandla Msimanga
Dept of Physics, TUT / IBA Division, iThemba LABS
SAIP 2025, 10 July, WITS University

## Slide 2
Ion beams in materials research
Research problem
Measurement of collision parameters
  Stopping force (stopping power)
  X-ray production cross sections
Talk outline

## Slide 3
Prof M Msimanga, Physics Dept, TUT- 2025
Quite often the purpose of Ion Beam Analysis (IBA) in materials research is to
Identify
what atomic species are in a given sample ?
Quantify
how much of each is present ?
Give a depth profile
what is the depth distribution of the identified atomic species ?
There are a number of nuclear analytical techniques that are based on energetic ion beams from particle accelerators, each technique with its own particular advantage
The list includes PIXE, RBS, NRA, MeV SIMS, PIGE and ERDA
Ion beams in materials research

## Slide 4
Instrumentation

## Slide 5
Te - L shell lines
Zn - K shell lines
Example of a PIXE spectrum of a ZnTe/PET film analysed using 2.4 MeV H+ ions
PIXE

## Slide 6
Knowledge of the energy loss rate facilitates film thickness measurement
In RBS and ERDA………..
∆x

## Slide 7
Example…….
SiO2/Si3N4 film thickness measurement and stoichiometric analysis via RBS using 1.6 MeV He+ ions
SiO2 (105 nm)
Si3N4 (75 nm)
Backing membrane

## Slide 8
Existing ion atom interaction theories fare quite well when the collision pair is highly asymmetric in terms of mass
Research problem
Z1 << Z2
Pure Coulomb potential
Z 1 ≤ Z2
screening by orbital electrons cannot be neglected
Screened potentials

## Slide 9
Stopping force: Existing theoretical and semi-empirical formulations deviate by as much as 20 – 40% when it comes to predicting stopping force in heavy ion atom collisions
Research problem
https://www-nds.iaea.org/stopping/tuples/Si-SiO2
IBA energy region
Electronic stopping force of Si in SiO2

## Slide 10
II. X-ray production cross sections: Theoretical predictions of heavy ion induced X-ray production cross sections are generally at variance with experiment, especially for Z1/Z2 ≥ 0.4 collision pairs
X-ray production cross sections σX(E) are required to calculate elemental concentrations from X-ray yields.
There is a need for accurate databases of S(E) and σX(E) values (among other factors) for accurate IBA data analysis
More experimental data for validation of theory/semi-empirical formulations, especially for heavy ions (i.e. Z > 6)

## Slide 11
RBS.
PIXE
..centred around the 6 MV Tandem [High Voltage Engineering] at iThemba LABS TAMS
control room
NMP chamber
Timing detector
ToF-ERDA set up
Heavy Ion – ToF ERDA
NEC Alphatross He ion source
860C SNICS ion source : H - Au
Measurement of heavy ion-atom collision parameters:

## Slide 12
T1, T2 – Microchannel Plate timing detectors
I. Heavy ion stopping force measurement for IBA applications
Measurement of stopping force using Time of Flight spectrometry at iThemba LABS
e.g. Cu
e.g. SiO2
e.g. Au

## Slide 13
Measurement of stopping force using ToF spectrometry
ToF and recoil energy E are measured in coincidence
ToF detector measures incident energy E1, PIPS detector measures exit energy E2
1
2

## Slide 14
ToF projections are continued along the energy axis to give a continuous stopping force curve
The energy loss is then determined by
where m denotes the mass of the recoil ion. The stopping force S(E) is then calculated as
at an average energy Eav given by

## Slide 15
Comparison with theory
Experimental data is compared to predictions from:
SRIM
  Stopping and Range of Ions in Matter (www.srim.org)
DPass
  Binary Stopping Theory (www.sdu.dk/DPASS)
CasP
  Convolution approximation for Swift Particles (http://www.casp-program.org/)

## Slide 16
Stopper foil -> Ti
Some results from iThemba LABS…..

## Slide 17
Results………..
Carbon
Oxygen
Magnesium
Copper

## Slide 18
Stopper foils -> SiO2 and HfO2

## Slide 19
from Barradas et. al NIMB 360 (2015) 90-96,
IAEA Coordinated Research Project
Stopping force through the backing Si3N4 membrane
2007
2013
2015

## Slide 20
Stopping force measurement results for Si and Cu ions
Data now part of the IAEA stopping force database
https://www-nds.iaea.org/stopping/tuples/Si-SiO2

## Slide 21
II. X-ray production cross sections for heavy ion PIXE
Collisions between heavy ions are characterised by multiple ionisation effects in both the target and projectile atoms:
Multiple ionisation leads to changes in:
  X-ray line intensity ratios (e.g. Γα/Γβ)
  Characteristic X-ray energies
  Fluorescence yields ωo
As a result, X-ray production cross sections (σx) in heavy ion collisions deviate from those of singly ionised cases
Existing X-ray ionisation theories (e.g. PWBA, ECPSSR) do not fully account for these effects

## Slide 22
XPCS measurements for heavy ion PIXE
X-ray yield
Backscattering yield
Sample parameters
Energy loss correction factor
X-ray detector efficiency
Backscattering cross section
projectile (m, Z)

## Slide 23
Some XPCS outputs from iThemba LABS
For high velocity and highly asymmetric collisions, i.e. Z1/Z2 << 0.5, ECPSSR theory describes the direct ionisation (DI) mechanism fairly well
As Z1 increases, for nearly symmetric collisions (i.e. Z1/Z2 -> 0.5), other effects come into play that are not so well described by theory

## Slide 24
Some XPCS outputs from iThemba LABS
Similar to the C -> Ta case
Similar to the Si -> Ru case

## Slide 25
An attempt at predictive formulations……
Heavy ion (HI) induced XPCS compared to proton (p) cross sections:

## Slide 26
Some XPCS outputs from iThemba LABS
Semi-empirical calculation vs experiment for O -> Bi collision system
2023

## Slide 27
Experiment shows that, theoretical predictions of heavy ion stopping force deviate from experiment by up to 20% - 40% at times.
In heavy ion induced XPCS the extent of deviations increases as the colliding particle masses increase, especially at low ion velocities
Because of the huge number of possible ion-target-energy permutations, more data intensive approaches need to be explored
Conclusion and future outlook
E.g. IAEA database for machine learning approaches

## Slide 28
End, thank you