## Slide 1: Transport properties of Co2Ti1−xCrxAl Heusler compounds
M. Mulibana, A.R.E. Prinsloo, C.J. Sheppard, B.S. Jacobs
Chromium Research Group (CRG), Department of Physics, University of Johannesburg (UJ)
Email address: mureim@uj.ac.za

## Slide 2: Outline
Introduction
Motivation and Aim
Methodology:
  Synthesis
  Characterization
Results:
  Temperature dependence of resistivity (four-point probe configuration)
  Density of states (DOS)
Conclusion

## Slide 3: Introduction: Structure
Figure 1. Crystal structure of an X2YZ Heusler compound. The blue, pink, and green spheres represent atoms at the X site (8c), Y site (4b) and Z site (4a). The Figure was generated using VESTA [1].
[1] K. Momma and F. Izumi, J. Appl. Crystallogr. 44 (2011) 1272.
Full-Heusler compounds
X2YZ chemical composition.
X and Y elements are transition metals and Z is a main group element.
Consist of four interpenetrating FCC lattices.
Occupied Wyckoff positions are 8c (0.25, 0.25, 0.25), 4b (0.5, 0.5, 0.5) and 4a (0, 0, 0)
Space group , L21.
X
Y
Z

## Slide 4
1903
Discovery of ferromagnetism in Cu2MnAl by Fritz Heusler [1].
2003
Prediction of half-metallic property in Co2MnZ (Z = Al, Sn) by Ishida et al. [2] and Kübler et al. [3] using density of state (DOS) and band structure calculation.
1983
Observation of a large negative magnetoresistance effect in Co2Cr0.6Fe0.4Al by Block et al. [4]
2003-2025
The search for new and unique properties for X2YZ with X = Co, using both theoretical and experimental techniques for spintronic application.
[1] T. Graf et al., Prog. Solid State Chem. 39 (2011) 1.
[2] S. Ishida et al., J. Phys. Soc. Jpn. 48 (1980) 814.
[3] J. Kübler et al., Phys. Rev. B. 28 (1983) 1745.
[4] T. Block et al., J. Solid State Chem. 176 (2003) 646.
Introduction: History

## Slide 5
Half-metallic ferromagnets
Figure 2. Schematic illustration of the density of states of (a) a metal, (b) a metal (spin resolved), (c) a ferromagnet, and (d) a half-metallic ferromagnet.
[1] T. Graf et al., Prog. Solid State Chem. 39 (2011) 1.
(a)
(b)
(c)
(d)
Metal
(Total DOS)
Metal
(Spin resolved)
ferromagnet
(Spin resolved)
Half-metallic
ferromagnet
(Spin resolved)

## Slide 6
Half-metallic ferromagnets
Figure 3. (a)-(c) Band structure and total density of states of Co2CrAl for spin up and spin down. Reproduced with permission from [1].
[1] K. Qu et al., AIP Advances, 14 (2024) 055311.

## Slide 7
The temperature dependence of DC electrical resistivity is expressed as:
,
Temperature dependent resistivity
[1] Chatterjee et al., J. Phys.: Condens. Matter. 34 (2022) 013001.
Residual resistivity (temperature independent)
Electron-electron scattering (.
Electron-magnon scattering.
Electron-Phonon scattering ()

## Slide 8
Electron-Magnon scattering
(A) Typical ferromagnets:
One-magnon scattering
(B) Half-metallic ferromagnets:
Two-magnon scattering
Manifests as at , where is the Curie temperature [1].
Manifests as at and at , where is the Curie temperature [1].
[1] V. Y. Irkhin and M. I. Katsnel’son, Phys.-Usp. 37 (1994) 659.

## Slide 9
Motivation:
Most of the studies reporting half-metallic properties in Co2YZ are based on theoretical structures.
Is it possible to experimentally synthesize a half-metallic Co2YZ Heusler compound?
Aim:
Synthesize and experimentally investigate the half-metallic property of Co2Ti1−xCrxAl.
Aim and Motivation
Co2TiAl has
Co2CrAl has
?

## Slide 10
Synthesis of samples
Arc-melting method was used to synthesize Co2Ti1−xCrxAl compounds using high purity elements (>99.9 %).
Melting was done in an arc furnace under an argon (Ar) atmosphere.
The elements were melted with crushing in between melts to promote homogeneity.
Resulting ingots were cut into specific geometries using spark erosion for characterization.

## Slide 11
Characterization
The samples were characterized using x-ray powder diffraction (XRD) for structural analysis.
Transport properties were probed by measuring the temperature dependence of resistivity using the four-point probe method.
Electronic properties were investigated using density of state (DOS) calculations using GPAW [1] and CIF from Rietveld refinement:
  Plane wave basis (PW) with cut-off energy of 500 eV on a 15×15×15 k-point grid [2].
  Generalized Gradient Approximation within the Perdew-Burke-Ernzerhof (PBE) formulation [3].
[1] J. J. Mortensen et al., J. Chem. Phys. 160 (2024) 092503.
[2] J. P. Perdew et al., Phys. Rev. Lett. 77 (1996) 3865.
[3] J. D. Pack and H. J. Monkhorst, Phys. Rev. B. 16 (1977) 1748.

## Slide 12
Figure 4. Rietveld refined room temperature XRD data for Co2Ti1−xCrxAl with (a) x = 0, and (b) x = 0.25. The open black circle (IObs) denotes the experimental data, solid red line (ICal) is the calculated data, blue line is the difference between IObs and ICalc, the black solid vertical lines denote the Bragg positions belonging to L21 () phases.
X-ray diffraction

## Slide 13
X-ray diffraction
Figure 5. Rietveld refined room temperature XRD data for Co2Ti1−xCrxAl with (c) x = 0.50, (d) x = 0.75, and (e) x = 1. The open black circle (IObs) denotes the experimental data, solid red line (ICal) is the calculated data, blue line is the difference between IObs and ICalc, the black and pink solid vertical lines denote the Bragg positions belonging to L21 () and monoclinic () phases, respectively.

## Slide 14
Figure 6. Crystal structure of (a) single-phase and (b) binary-phase Co2Ti1−xCrxAl compound. Figures were generated using VESTA software [1].
(a) Single Phase:
[1] K. Momma and F. Izumi, J. Appl. Crystallogr. 44 (2011) 1272.
(b) Binary Phase:
X-ray diffraction

## Slide 15
Temperature dependent resistivity
Figure 7. Temperature dependence of resistivity of Co2TiAl measured from 4 K to 300 K.
Region I (Green): |  |  | 
(μΩ cm | (μΩ cm K−1/2) | A (μΩ cm K−2) | B (μΩ cm K−9/2)
23.9(1) | - | 2.4(1) | 3.3(0)
Region II (Blue): |  |  | 
(μΩ cm) | a (μΩ cm K−2) | b (μΩ cm K−7/2) | c (μΩ cm K−1)
21.8(1) | 2.5(3) | 2.0(1) | -
Region III (Red): |  |  | 
(μΩ cm) | a (μΩ cm K−2) | b (μΩ cm K−7/2) | C (μΩ cm K−1
23.2(6) | - | - | 0.457(1)
 |  | A (μΩ cm K−2) | B (μΩ cm K−9/2)
23.9(1) | - |  | 
 | a (μΩ cm K−2) | b (μΩ cm K−7/2) | c (μΩ cm K−1)
21.8(1) |  |  | -
 | a (μΩ cm K−2) | b (μΩ cm K−7/2) | C (μΩ cm K−1
23.2(6) | - | - | 0.457(1)

## Slide 16
Figure 8. Temperature dependence of resistivity of Co2Ti0.75Cr0.25Al measured from 4 K to 450 K.
Region I (Green): |  |  | 
(μΩ cm | (μΩ cm K−1/2) | A (μΩ cm K−2) | B (μΩ cm K−9/2)
111.3(2) | 0.09(5) | 3.3(8) | 2.1(6)
Region II (Blue): |  |  | 
(μΩ cm) | a (μΩ cm K−2) | b (μΩ cm K−7/2) | c (μΩ cm K−1)
110.3(8) | - | 4.8(3) | 7.7(2)
 |  | A (μΩ cm K−2) | B (μΩ cm K−9/2)
111.3(2) | 0.09(5) |  | 
 | a (μΩ cm K−2) | b (μΩ cm K−7/2) | c (μΩ cm K−1)
110.3(8) | - |  | 
Temperature dependent resistivity

## Slide 17
Figure 9. Temperature dependence of resistivity of Co2Ti0.5Cr0.5Al measured from 4 K to 450 K.
Region I (Green): |  |  | 
(μΩ cm | (μΩ cm K−1/2) | A (μΩ cm K−2) | B (μΩ cm K−9/2)
119.6(4) | - | 3.22(3) | -
Region II (Blue): |  |  | 
(μΩ cm) | a (μΩ cm K−2) | b (μΩ cm K−7/2) | c (μΩ cm K−1)
112.7(1) | 4.5(2) | - | 0.110(2)
Region III (Red): |  |  | 
(μΩ cm) | a (μΩ cm K−2) | b (μΩ cm K−7/2) | C (μΩ cm K−1
109.3(3) | - | - | 0.135(1)
 |  | A (μΩ cm K−2) | B (μΩ cm K−9/2)
119.6(4) | - |  | -
 | a (μΩ cm K−2) | b (μΩ cm K−7/2) | c (μΩ cm K−1)
112.7(1) |  | - | 0.110(2)
 | a (μΩ cm K−2) | b (μΩ cm K−7/2) | C (μΩ cm K−1
109.3(3) | - | - | 0.135(1)
Temperature dependent resistivity

## Slide 18
Figure 10. Temperature dependence of resistivity of Co2Ti0.25Cr0.75Al measured from 4 K to 450 K.
Region I (Green): |  |  | 
(μΩ cm | (μΩ cm K−1/2) | A (μΩ cm K−2) | B (μΩ cm K−9/2)
106.9(0) | - | 1.04(1) | -
Region II (Blue): |  |  | 
(μΩ cm) | a (μΩ cm K−2) | b (μΩ cm K−7/2) | c (μΩ cm K−1)
97.02(1) | 2.92(6) | 3.02(4) | 0.194(1)
Region III (Red): |  |  | 
(μΩ cm) | a (μΩ cm K−2) | b (μΩ cm K−7/2) | C (μΩ cm K−1
108.5(2) | - | - | 0.217(2)
 |  | A (μΩ cm K−2) | B (μΩ cm K−9/2)
106.9(0) | - |  | -
 | a (μΩ cm K−2) | b (μΩ cm K−7/2) | c (μΩ cm K−1)
97.02(1) |  |  | 0.194(1)
 | a (μΩ cm K−2) | b (μΩ cm K−7/2) | C (μΩ cm K−1
108.5(2) | - | - | 0.217(2)
Temperature dependent resistivity

## Slide 19
All synthesized Co2Ti1−xCrxAl (x = 0, 0.25, 0.5, 0.75) compounds are metallic.
For Co2TiAl, two-magnon scattering dominates at , and one-magnon scattering is dominant at .
Significant amount of weak localization effect is observed for x = 0.25 at , with one-magnon scattering dominating over the two-magnon scattering term.
One-magnon scattering dominates for Co2Ti0.5Cr0.5Al below .
Co2Ti0.25Cr0.75Al shows one-magnon scattering at and two-magnon scattering at .
Temperature dependent resistivity

## Slide 20
Temperature dependent resistivity
Figure 11. Temperature dependence of resistivity of Co2CrAl 78 K to 480 K.
for Co2CrAl increases linearly with decreasing temperature between 78 K and 330 K.
.
Temperature coefficient resistivity (TCR) of .
The linear behaviour suggests that the compound behaves like a spin-gapless semiconductor [1].
[1] Rani et al., J. Appl. Phys. 128 (2020) 220902.

## Slide 21
Figure 12. (a) Schematic illustration of the density of states of a Half-metal (HM) and spin-gapless semiconductor (SGS) [1]. (b) Spin-resolved density of state of Co2CrAl calculated using GPAW.
HM
SGS
(a)
[1] Rani et al., J. Appl. Phys. 128 (2020) 220902.
Temperature dependent resistivity

## Slide 22
Summary
Co2Ti1−xCrxAl (x = 0, 0.25, 0.5, 0.75, 1) were synthesized using the arc-melting method.
Rietveld refinement analysis revealed disordered single phase structures for x = 0, 0.25, and x = 1 and disordered binary phases were observed for x = 0.5, and x = 0.75.
demonstrates metallic behaviour for x ≤ 0.75.
At , a dominant two-magnon scattering process is observed for x = 0.
At , a two-magnon scattering process is observed only for x = 0.75.
Co2CrAl demonstrates spin-gapless semiconducting behaviour with a negative temperature coefficient resistivity (TCR) , however, density of state (DOS) calculations do not show this behaviour.

## Slide 23
Acknowledgement
Financial aid from the SANRF (Grant no. SHUG2204041966 and 138329) and the UJ/FRC are acknowledged.
University of Johannesburg (UJ) URC and FRC (Grant No. 282810 and 083135).
Use of NEP Cryogenic Physical Properties Measurement System at UJ, obtained with financial support from SANRF (Grant no: 88080) and UJ, is acknowledged.
The use of the Spectrum Facility in the Faculty of Science (FOS) at UJ is acknowledged.

## Slide 25
Supplementary information

## Slide 26
Density functional theory (DFT) calculations were performed using GPAW [1]. The code is based on Projector augmented wave (PAW) method. The generalized gradient approximation (GGA) within the Perdew-Burke-Ernzerhof (PBE) formulation [2] was used to treat the electronic exchange and correlation effects. The wave functions were expanded using plane wave (PW) basis with a cutoff energy of 500 eV. A k-point mesh of the Monkhorst-Pack type [3] was used with 15×15×15 grid sample in the irreducible Brillouin zone (IBZ).
[1] Mortensen J J et al., (2024), GPAW: An open Python package for electronic structure calculations J. Chem. Phys. 160
[2] Perdew J P et al., (1996), Generalized Gradient Approximation Made Simple, Phys. Rev. Lett. 77 3865–8
[3] Pack J D and Monkhorst H J, (1977), special points for Brillouin-zone integrations, Phys. Rev. B 16 1748–9
DFT calculation details

## Slide 27
Table 1. Crystal structure parameters and refinement parameters obtained from Rietveld analysis of Co2Ti(1−x)Cr(x)Al (x = 0, 0.25, 0.50, 0.75, 1) XRD data using a cubic () structure and monoclinic () structure.
X-ray diffraction
x | a (Å) = b (Å) = c (Å) | a (Å) = b (Å) = c (Å) |  |  |  | α (°) = β (°) = γ (°) |  |  | V (Å3) | Rwp | Rexp | Rexp
0 | 5.85 | 5.85 |  |  |  | 90.00 |  |  | 200.14 | 9.65 | 10.60 | 10.60
0.25 | 5.83 | 5.83 |  |  |  | 90.00 |  |  | 198.20 | 10.20 | 10.74 | 10.74
0.50 | 5.81 | 5.81 |  |  |  | 90.00 |  |  | 195.86 | 10.14 | 11.27 | 11.27
0.75 | 5.78 | 5.78 |  |  |  | 90.00 |  |  | 192.75 | 10.07 | 11.57 | 11.57
1 | 5.73 | 5.73 |  |  |  | 90.00 |  |  | 188.60 | 10.85 | 11.19 | 11.19
x | a (Å) | b (Å) | b (Å) | c (Å) | α (°) |  | β (°) | γ (°) | V (Å3) | Rwp |  | Rexp
0.50 | 19.46 | 5.66 | 5.66 | 4.28 | 90.00 |  | 97.69 | 90.00 | 467.51 | 10.14 |  | 11.27
0.75 | 19.43 | 5.65 | 5.65 | 4.27 | 90.00 |  | 97.76 | 90.00 | 464.51 | 10.07 |  | 11.57
x | a (Å) = b (Å) = c (Å) | a (Å) = b (Å) = c (Å) |  |  |  | α (°) = β (°) = γ (°) |  |  | V (Å3) | Rwp | Rexp | Rexp
0 | 5.85 | 5.85 |  |  |  | 90.00 |  |  | 200.14 | 9.65 | 10.60 | 10.60
0.25 | 5.83 | 5.83 |  |  |  | 90.00 |  |  | 198.20 | 10.20 | 10.74 | 10.74
0.50 | 5.81 | 5.81 |  |  |  | 90.00 |  |  | 195.86 | 10.14 | 11.27 | 11.27
0.75 | 5.78 | 5.78 |  |  |  | 90.00 |  |  | 192.75 | 10.07 | 11.57 | 11.57
1 | 5.73 | 5.73 |  |  |  | 90.00 |  |  | 188.60 | 10.85 | 11.19 | 11.19
x | a (Å) | b (Å) | b (Å) | c (Å) | α (°) |  | β (°) | γ (°) | V (Å3) | Rwp |  | Rexp
0.50 | 19.46 | 5.66 | 5.66 | 4.28 | 90.00 |  | 97.69 | 90.00 | 467.51 | 10.14 |  | 11.27
0.75 | 19.43 | 5.65 | 5.65 | 4.27 | 90.00 |  | 97.76 | 90.00 | 464.51 | 10.07 |  | 11.57

## Slide 28
Temperature dependent magnetization
Figure 13. Field-cooled (FC) and zero-field cooled (ZFC) temperature dependence of magnetic susceptibility (), inverse magnetic susceptibility () for Co2Ti(1−x)Cr(x)Al with (a) x = 0 and (b) x = 0.25.

## Slide 29
Temperature dependent magnetization
Figure 14. Field-cooled (FC) and zero-field cooled (ZFC) temperature dependence of magnetic susceptibility (), inverse magnetic susceptibility () for Co2Ti(1−x)Cr(x)Al with (c) x = 0.5 and (d) x = 0.75.

## Slide 30
Temperature dependent magnetization
Figure 14. Field-cooled (FC) and zero-field cooled (ZFC) temperature dependence of magnetic susceptibility (), inverse magnetic susceptibility () for Co2Ti(1−x)Cr(x)Al with (e) x = 1 and (f) Curie temperature (TC), paramagnetic Curie temperature (θCW) and effective magnetic moment (μeff) as a function of Cr concentration.

## Slide 31
Temperature dependent magnetization
Table 2. Critical temperature (TC) obtained from fitting with a Voigt function, fitting parameters , , and , and the effective moment ().
Compound (x) | TC (K) | (10−8 m3mol−1) | (K) | (10−6 m3Kmol−1) | ()
0 | 119.0(1) | 6.0(1) | 144.5(8) | 3.36(1) | 1.5(1)
0.25 | 334.3(4) | - | 371.9(5) | 6.92(1) | 2.0(1)
0.50 | 414(1) | - | 435.7(7) | 7.5(1) | 2.2(2)
0.75 | 412.8(1) | - | 424(3) | 10.21(3) | 2.1(1)
1.00 | 327.0(3) | - | 337.8(4) | 17.85(2) | 3.4(1)
Compound (x) | TC (K) |  |  |  | 
0 | 119.0(1) | 6.0(1) | 144.5(8) | 3.36(1) | 1.5(1)
0.25 | 334.3(4) | - | 371.9(5) | 6.92(1) | 2.0(1)
0.50 | 414(1) | - | 435.7(7) | 7.5(1) | 2.2(2)
0.75 | 412.8(1) | - | 424(3) | 10.21(3) | 2.1(1)
1.00 | 327.0(3) | - | 337.8(4) | 17.85(2) | 3.4(1)