## Slide 1
DFT-based evaluation of Li2MnO3 as a promising cathode coating material for lithium-ion batteries
M.Z. Kgasago1, K.W. Phoshoko2, P. E. Ngoepe1 and R.S. Ledwaba1
1. Materials Modelling Centre, School of Physical and Mineral Sciences
University of Limpopo, Private Bag x 1106, Sovenga, 0727, South Africa
2. Data Intensive Research Initiative of South Africa, Council for Scientific and Industrial Research,
P.O. Box 395, Pretoria, 0001, South Africa
Email: Kgasagomogau@gmail.com

## Slide 2: Introduction
A perfect cathode material for lithium-ion batteries does not yet exist [1,2].
LiCoO2
LiFePO4
LiMn2O4
J Guo, S Li, B Zhu, H Zhang, X Gao, Y Wu, S Zhang, N Wen, X Wang, Y Lai, Z Zhang, Chemical Engineering Journal, 471, 1-10, (2023).
J Xu, S Zhu, Z Xu, H Zhu, Computational Materials Science, 229, 1-7, (2023).
LiMn2O4’s spinel structure has 3D lithium pathways and offers abundance, low cost, and good thermal stability [2].

## Slide 3: Drawbacks of spinel
The spinel LiMn2O4 presents the following key challenges as a cathode material:
Surface coating [3]
Doping [4]
Core-shell design [4]
Many methods have been introduced to modify the properties and morphology of this structure to enhance its stability and performance.
Jahn–Teller distortion causes structural instability [2]
Capacity fading due to transition metal dissolution [2]
2. J Xu, S Zhu, Z Xu, H Zhu, Computational Materials Science, 229, 1-7, (2023).
3. NM Jobst, G Gabrielli, P Axmann, M Hölzle, M Wohlfahrt-Mehrens, Journal of The Electrochemical Society, 168, 1-8, (2021).
4. C Tomon, S Sarawutanuku, N Phattharasupakun, S Duangdangchote, P Chomkhuntod, N Joraleechanchai, P Bunyanidhi, M Sawangphruk, 552, 1-12, 2022

## Slide 4: A core-shell design
Spinel Fd-3m
Layered C/2m
The advantages of the core-shell design:
Mitigate phase transition [5].
Minimize unwanted reactions.
Prevent electrode-electrolyte interactions.
LiMn2O4
Li2MnO3
5. Xu J, Zhu S, Xu Z, Zhu H, Computational Material Science, 229, 1-7, (2023).
In this study, we use density functional theory (DFT) to investigate the compatibility of Li2MnO3 as a shell material for LiMn2O4

## Slide 5: Methodology
Density functional theory (DFT) [6]
Vienna Ab-initio Simulation Package (VASP) code [7]
Energy cut-off: 500 eV k-points-
LiMn2O4: 5x5x5 Li2MnO3: 4X4X4
Convergence test
U-parameter
LiMn2O4=4 Li2MnO3=5
GGA+U [8]
FM vs AFM
Spin configurations
Structural properties
Electronic properties
6. W Kohn, LJ Sham, Physical Review, 140, A1133-A1138, (1965).
7. G Kresse, J Hafner. Physical Review B, 49 14251 – 14269 (1994)
8. J P Perdew, K Burke, and M Ernzerhof, Physical Review Letter, 77, 3865 (1996).

## Slide 6: Structural properties
For both systems, the AFM configuration consistently provides better agreement with experimental lattice parameters compared to the FM configuration.
9. Y Idemoto, K Horiko, K Ui, N Koura , Electrochemistry, 72, 10, 680-687, (2004).
10. P Strobel, B Lambert-Andron, Journal of Solid-State Chemistry, 75, 90-98, (1988).
System | Lattice parameters (Å) |  | 
 | GGA+U |  | 
 | FM | AFM | Experimental
LiMn2O4 f-3m | 8.35 | 8.33 | 8.24 [9]
Li2MnO3 C/2m | a=5.01 b=8.65 c=5.08 | a=4.95 b=8.54 c=5.03 | a=4.94 [10] b=8.53 c=5.05
Li2MnO3
LiMn2O4
AFM
FM

## Slide 7: Bond lengths
2.178
2.179
1.994
1.941
1.976
1.948
1.927
1.971
1.938
1.950
1.902
1.930
1.925
1.918
1.925
1.925
1.918
1.925
1.918
1.918
1.930
1.926
1.918
Mn3+
Mn4+
Mn4+
Mn4+
Li2MnO3
LiMn2O4
Material | Valence State | Average Bond lengths (Å)
LiMn2O4 | Mn3+ | 2.0325
 | Mn4+ | 1.9418
Li2MnO3 | Mn4+ | 1.9235
In LiMn2O4, Mn3+–O bonds are longer due to Jahn–Teller distortion, causing structural instability.
Li2MnO3 shows uniform Mn4+–O bond lengths, reflecting a more stable structure.

## Slide 8: Magnetic Behavior of Mn
Material | Valence State | Magnetic Moments (µB)
LiMn2O4 | Mn3+ | 3.8
 | Mn4+ | 3.0
Li2MnO3 | Mn4+ | 3.1
Spinel
Layered
Electrolyte
LiMn2O4 shows two distinct magnetic moments, confirming Mn3+/Mn4+ coexistence.
Li2MnO3 shows uniform moments, consistent with Mn4+.
The uniform Mn⁴⁺ coating acts as a barrier between the spinel core and the electrolyte, preventing direct contact and thereby suppressing Mn dissolution.

## Slide 9: Density of states
LiMn2O4 has a small band gap (~0.5 eV), classified as a semiconductor.
Li2MnO3 has a wider band gap (~2.1 eV), also classified as a semiconductor.
LiMn2O4
Li2MnO3

## Slide 10: Diffusion pathways
LiMn2O4
Li2MnO3

## Slide 11: Conclusion
This study aimed to assess the compatibility of Li2MnO3 as a shell material for stabilizing a LiMn2O4 spinel core using DFT.
Structural analysis showed that LiMn2O4 suffers from Jahn–Teller distortion, while Li2MnO3 remains structurally stable.
Magnetic moments confirmed Mn3+/Mn4+ disorder in the core and uniform Mn4+ states in the shell.
DOS results showed that Li2MnO3 is a wide-gap semiconductor, helping reduce unwanted surface redox activity.
The layered Li2MnO3 shell will potentially act as a barrier between the spinel core and the electrolyte, helping suppress Mn dissolution and enhance cathode stability.

## Slide 12: Acknowledgements

## Slide 13: Thank You